Üst Kretase Yaşlı Bazaltlarda (Trabzon/Türkiye) Fiziksel, Mekanik

ve Kimyasal Özellikler ile Bozunma Derecesi Arasındaki İlişkiler

Selçuk Alemdağ1 ve Zülfü Gürocak2

1 Gümüşhane Üniversitesi Jeoloji Mühendisliği Bölümü, 29000 Gümüşhane

(E-posta: selcukalemdag@gmail.com)

2 Fırat Üniversitesi, Jeoloji Mühendisliği Bölümü, 23119 Elazığ

Bu çalışmada farklı bozunma derecesine sahip bazaltlarda, bozunmanın fiziksel, mekanik ve kimyasal özellikler üzerindeki etkileri incelenmiştir. Bazaltlardan ISRM tarafından önerilen bozunma sınıflamasına uygun olarak farklı bozunma derecesine sahip örnekler derlenmiş ve bu örneklerin fiziksel, mekanik ve kimyasal özellikleri belirlenmiştir. Bazaltlarda birim hacim ağırlık, su emme, porozite, tek eksenli sıkışma dayanımı, Schmidt geri sıçrama değeri, P dalga hızı, RQD, eklem sıklığı ve kimyasal ayrışma indeksleri ile bozunma derecesi arasındaki ilişkiler incelenmiştir. Yapılan istatistiksel değerlendirmelere göre, bazaltlarda bozunma derecesi ile tek eksenli sıkışma dayanımı, P dalga hızı ve Ruxton Oranı (R) arasında kuvvetli negatif bir ilişki,  Vogt Oranı (V) arasında ise kuvvetli pozitif bir ilişki belirlenmiştir. Bu ilişkiler, ISRM tarafından önerilen bozunma derecesine göre tanımlanan bazaltların tek eksenli sıkışma dayanımı, P dalga hızı ve ana oksit oranları değer aralıklarının tahmin edilebilmesi açısından yarar sağlayacaktır.

Anahtar Sözcükler: bazalt, bozunma derecesi, fiziksel özellik, mekanik özellik, kimyasal özellik

The Relationships Between Mechanical, Chemical Properties and  Weathering Degree in the Upper Cretaceous Basalts (Trabzon/Turkey)

Selçuk Alemdağ1 & Zülfü Gürocak2

1 Gümüşhane Üniversitesi Jeoloji Mühendisliği Bölümü, TR−29000 Gümüşhane, Türkiye

(E-mail: selcukalemdag@gmail.com)

2 Fırat Üniversitesi, Jeoloji Mühendisliği Bölümü, TR−23119 Elazığ, Türkiye

In this study, effects of weathering degree on the physical, mechanical and chemical properties of basalts having different weathering degree were examined. Basalts having different weathering degree were collected in accordance with the weathering classification of ISRM and physical, mechanical and chemical properties of these samples were determined. The relationships between unit weight, water absorption, porosity, uniaxial compressive strength, Schmidt rebound value, compressive wave velocity, RQD, joint frequency, chemical alteration index and weathering degree were evaluated in basalts. According to statistical evalutions,  strong negative relationships were found between the weathering degree and uniaxial compressive strength, compressive wave velocity, Ruxton ratio. The relationship between weathering degree and Vogt ratio was strong positive. These relationships will be useful for predicting ranges of uniaxial compressive strength, compressive wave velocity and main oxide percentage for the basalts which are described accordance with the weathering classification of ISRM.

Key Words: basalt, weathering degree, physical protery, mechanical property, chemical property