Bahçeli Antik Roma Havuzunun Mühendislik Özellikleri

Mustafa Korkanç1 ve Sevil Tokgöz2

1 Niğde Üniversitesi, Jeoloji Mühendisliği Bölümü, 51290 Niğde

(E-posta: mkorkanc@nigde.edu.tr)

2 Niğde Üniversitesi, Fen Bilimleri Enstitüsü, 51290 Niğde

Niğde yöresinde geçmiş dönemlerde değişik medeniyetler tarafından inşa edilmiş çeşitli özellikte kültürel yapılar bulunmaktadır. Bunların bir kısmı oldukça büyük ve önemli yapılar olup, sanatsal, kültürel ve estetik özellikleri de oldukça ilginçtir. Roma Havuzu da bunlardan biri olup, Niğde’nin 17 km güneyinde Adana-Kayseri yolunun 1 km kuzeyindeki Bahçeli kasabasında bulunmaktadır. Yapı, Roma dönemi mermer sanatının 23x66x2,5 m boyutundaki ender bir örneğidir. Tamamen toprak altında bulunan havuz, 1960 yılında tesadüfen ortaya çıkarılmıştır. Gezginci Roma İmparatorlarının önemli bir mesire yeri olan antik havuzun yapımında iri bloklu mermerler yapı taşı olarak kullanılmıştır. Bu çalışmada antik havuzunun bulunduğu bölgenin jeolojik özellikleri ile burada kullanılan taşların jeomekanik özelliklerine yönelik değerlendirmeler yapılmıştır. Bu kapsamda öncelikle petrografik incelemeler ve XRD analizleri yapılmıştır. Taşların jeomekanik özelliklerinin belirlenmesine yönelik olarak kuru ve doygun birim ağırlık, ağırlıkça su emme, efektif porozite ve suda dağılmaya karşı duraylılık indeksi, P-dalga hızı ve tek eksenli basınç dayanımı deneyleri ile antik havuzun duvarlarında kullanılan mermerler üzerinde yerinde Schmidt çekici sertlik ölçümleri alınmıştır. Roma havuzunun bulunduğu alanda temel zeminini yeşil-beyazımsı marn ve kireçtaşı ile ardalanımlı, laminalı gri-kahverenkli çamurtaşı ara katkılarından oluşan Gökbez formasyonuna ait birimler oluşturmaktadır. Yapının bulunduğu alanda temel zemininin taşıma gücüne yönelik herhangi bir olumsuzluk gözlenmemiştir. Kullanılan mermerler içerisinde iri kristalli olanlarda yersel erimeler söz konusu olup, bunda atmosferik etkiler yanında kayacın oluşumundan kaynaklanan jeolojik sorunların etkili olduğu belirlenmiştir.

Anahtar Sözcükler: Niğde, jeoarkeoloji, roma havuzu, jeomekanik özellikler, mermer, ayrışma

Engineering Properties of the Bahçeli Ancient Roman Pool

Mustafa Korkanç1 & Sevil Tokgöz2

1Niğde Üniversitesi, Jeoloji Mühendisliği Bölümü, TR−51290 Niğde, Türkiye

(E-mail: mkorkanc@nigde.edu.tr)

2 Niğde Üniversitesi, Fen Bilimleri Enstitüsü, TR−51290 Niğde, Türkiye

In Nigde region, various cultural assets were built by different civilizations. A part of these are fairly huge buildings and their cultural, aesthetic and artistic properties are quite interesting. Roman Pool is situated 17 km south of the Nigde and 1 km north of the Adana-Kayseri road in Bahçeli district. It is a rare example of the marble art in Rome period that has a dimension of 23x66x2,5 m. The Pool that is wholly burried under soil was exposed coincidentally in 1960. Big block marbles were used as a building stone in the construction of Ancient Pool that is an important recreation spot for the voyager Roman Emperors. In this study, geological properties of the region where the antique pool is situated and geomechanical properties of the stones used for the pool were evaluated. For this purpose, petrographic investigations and XRD analysis were carried out. To determine the geochemical properties of the rocks; dry and saturated unit weight, water absorption, effective porosity and slake durability index, P-wave velocity and uniaxial compressive strength experiments and in-situ Schmidt hammer hardness measurements on marbles used for the walls of the antique pool were carried out. Ground is composed of greenish-whitish marl and limestone with alternation of laminated grey-brown colored mudstone units belonging to Gökbez formation. There is no problem observed for the bearing capacity of the basement that the building settled. Local meltings in coarse grained marbles were determined and besides the atmospheric effects, geological problems originated from the formation of the rocks were responsible for these meltings.

Key Words: Niğde, geoarchaeology, roma pool, geomechanical properties, marble, weathering